## Slide 1: Positronium migration
Radosław Zaleski
Maria Curie-Skłodowska University, Lublin, Poland

## Slide 2: Chapter 1
Positronium formation and thermalization
Ps
e+
e-

## Slide 3: Blob model
e+ emission from source (E ~ several hundred keV)
Rare central collisions → δe-
Non-central collisions → electron‑ion pairs in spherical spurs
Overlapping spurs (E < 3 keV) → cylindrical column of ionization
S.V. Stepanov, V.M. Byakov, J. Chem. Phys. 116, 14 (2002)
-
-
+
+
-
+
+
-
+
-
-
+
+
-
+
+
-
-
+
+
-
+
-
-
+
+
-
-
+
+
-
-
+
+
-
-
+
+
-
-
+
+
-
-
+
+
-
-
+
+
-
-
+
+
-
+
-
-
-
-
-
-
+
+
+
+
+
+
+
-
δe-
-
+
E ≈ 3 keV
e+

## Slide 4: Blob model
then
Positron diffusive-like movement (E < 0.5 keV) → spherical blob
Correlated positron-electron pair escapes blob (E < Ejon) → pre-Ps
Pre-Ps finds free volume (R > 0.1 nm) → Ps
-
-
+
+
-
+
+
-
+
-
-
+
+
-
+
+
-
-
+
+
-
+
-
-
+
+
-
-
+
+
-
-
+
+
-
-
+
+
-
-
+
+
-
-
+
+
-
-
+
+
-
-
+
+
-
+
-
-
-
-
-
-
+
+
+
+
+
+
+
-
δe-
-
+
+
-
+
-
-
-
-
-
+
+
+
+
+
-
-
-
+
+
+
+
-
-
e+
e-
E ≈ 3 keV
E ≈ 500 eV
10-20 nm
E ~ eV
Ps
S.V. Stepanov, V.M. Byakov, J. Chem. Phys. 116, 14 (2002)

## Slide 5: Blob model
No description if formation occurs in porous material!
(Especially blob and pre-Ps part)
-
-
+
+
-
+
+
-
+
-
-
+
+
-
+
+
-
-
+
+
-
+
-
-
+
+
-
-
+
+
-
-
+
+
-
-
+
+
-
-
+
+
-
-
+
+
-
-
+
+
-
-
+
+
-
+
-
-
-
-
-
-
+
+
+
+
+
+
+
-
δe-
-
+
+
-
+
-
-
-
-
-
+
+
+
+
+
-
-
-
+
+
+
+
-
-
e+
e-
E ≈ 3 keV
E ≈ 500 eV
10-20 nm
E ~ eV
Ps
S.V. Stepanov, V.M. Byakov, J. Chem. Phys. 116, 14 (2002)

## Slide 6: Positronium thermalization
Elastic Thermalisation Lifetime Analysis
C. Dauwe, B. Van Waeyenberge, D. Segers, T. Van Hoecke and J. Kuriplach, J. Radioanal. Nucl. Chem. 210, 293-308 (1996)
Phonon scattering
S. Mariazzi, A. Salemi and R.S. Brusa, Phys. Rev. B: Condens. Matter Mater. Phys. 78, 085428-085428 (2008)
Ps

## Slide 7: Positronium thermalization
Doppler spectroscopy
D.B. Cassidy, P. Crivelli, T.H. Hisakado, L. Liszkay, V.E. Meligne, P. Perez, H.W.K. Tom and A.P. Mills, Jr., Phys. Rev. A 81, 012715 (2010)

## Slide 8: Chapter 2
Positronium migration
Ps

## Slide 9: o-Ps migration
?
Ps
Ps formation
in mesopores
Ps
o-Ps migration from mesopores
to intergranular space
Ps
o-Ps (re)trapping and annihilation

## Slide 10: Open pores vs. closed pores
MCM-41
MSF

## Slide 11: Open pores vs. closed pores

## Slide 12: Template removal by MCM-41 heating in vacuum
~ 25%
Ps
Ps

## Slide 13: o-Ps intensity vs. oxygen pressure
Ps
Ps migration from
small to large pores in oxygen
SUPPRESSED
!

## Slide 14: Disagreement between experiment and model
S. Thraenert, E. M. Hassan, D. Enke, D. Fuerst, and R. Krause-Rehberg, physica status solidi (c) 4, 3819 (2007)
M. Sniegocka, B. Jasinska, T. Goworek, and R. Zaleski, Chem. Phys. Lett. 430, 351 (2006)
C. G. Fischer, M. H. Weber, C. L. Wang, S. P. McNeil, and K. G. Lynn, Physical Review B 71, 180102 (2005)
fotonic glass
MSSQ
porous silica
(polymer template)
Vycor
Numerous effects can cause Ps lifetime shortening, but
what causes its elongation?

## Slide 15: o-Ps lifetime vs. temperature
MELT
100 K
220 K
460 K
2,8 nm
3,4 nm
2,8 nm
3,4 nm
E

## Slide 16: o-Ps localization
2,8 nm
3,4 nm
460 K
100 K
LEVEL OCCUPATION
LEVEL OCCUPATION
LEVEL OCCUPATION
LEVEL OCCUPATION
Ps Ps Ps Ps
Ps
Ps
Ps
E

## Slide 17: o-Ps localization
M. Khaghani and A. A. Mehmandoost-Khajeh-Dad, Nucl. Instr. Meth. Phys. Res., 2017, 396, 11-17.

## Slide 18: Polymer-silica composites

## Slide 19: Micro- and mesopores
XAD7HP
O. Okay, Prog. Polym. Sci. 25 (2000) 711-779.
Davg
V
δD

## Slide 20: Amount of silica (PALS vs. LN2 adsorption)
25%
50%
75%
95%

## Slide 21: Amount of silica (PALS vs. LN2 adsorption)

## Slide 22: Chapter 3
The experiment

## Slide 23: Feasibility study
Position resolved PALS setup @ GiPS
Time of flight of positronium
formation and thermalization times
positronium final energy

## Slide 24: Feasibility study
“There is slight increase in number of counts at time expected for positronium migrating from the sample. Unfortunately it is still within statistical uncertainty. Despite the lack of statistics due to short beam time, we conclude the experiment to be feasible in general. “

## Slide 25: Feasibility study

## Slide 26: Epilogue
Can J-PET do this?